Stepwise ligand coordination and electronic stabilization in the nucleation of IRMOF-8

Aziza.Ergasheva1 and Umedjon Khalilov1,2

1) Institute of Ion-Plasma and Laser Technologies, Tashkent, Uzbekistan

2) University of Antwerp, Antwerp, Belgium

*) azizaabdujabborqizi@gmail.com

Metal-organic frameworks (MOFs) are widely studied for their high porosity and applications in catalysis, gas separation, and biology [1–4]. While MOF synthesis has been extensively investigated experimentally, the nucleation mechanisms remain poorly understood. In this study, we examine the nucleation of IRMOF-8 through reactive MD simulations, focusing on the stepwise coordination of ligands to the metal center (Fig. 1). The first ligand exhibits the highest binding energy (3.5 eV) with a metal charge of +0.91395, indicating a highly electron-deficient and reactive site. Subsequent ligand additions progressively reduce the binding energy (2.3, 2.3, 1.8, 1.7, and 1.4 eV for the 2nd–6th ligands) and lower the metal charge to +0.2966, reflecting enhanced electronic stabilization. These results provide detailed insight into the nucleation process of IRMOF-8, showing how ligand coordination gradually stabilizes the metal node and facilitates framework formation.

Figure 1. Step-by-step coordination process of the formation of the Mono-IRMOF-8 structure.

This study reveals how stepwise ligand coordination stabilizes the metal center and drives IRMOF-8 formation.

REFERENCES

[1]	O. M. Yaghi et al, Nature 423, 705 (2003).

[2]	Z. Lei et al., Advanced Energy Materials 8, 1801587 (2018).

[3]	X. Zhang et al., Electrochem. Energ. Rev. 2, 29 (2019).

[4]	Y. Deng et al., Biomater. Sci. 12, 3725 (2024).